CHAPTER 3 RESULTS AND DISCUSSIONS

3.0 Synthesis of Silk Fibroin / N, N’ methylene diacrylamide Biofilms

For the film-casting fabrication we used N, N’ methylene diacrylamide crosslinker and UV-irradiation, which is considered to be more versatile, practical and non-toxic process because limited amount of chemicals can be use and less parameters affects the quality of the final cast biofilms. The synthesis reactions were carried out at various wavelengths (254 nm and 365 nm) and crosslinker (C7H10N2O2) concentrations as shown in Table 3.1. In the following, the formation, swelling, biodegradability and morphologic properties of silk fibroin biofilms are discussed as depending on the synthesis parameters. Then, the blood clotting and platelet adhesion properties analyzed, discussed The aqueous silk fibroin concentrations obtained were 3% w/v, 4% w/v, 5% w/v, 6% w/v SF/ electrolyte solution but those ratios were not exact concentrations because an amount of distilled water diffused into the membrane during the dialysis process. After the dialysis process, concentrations of solution were decreased about half of the original concentration, 3%, 4%, 5%, and 6%, before dialysis process became 1.5%, 2%, 2.5%, 3%, after dialysis. Practical technique used to calculate the real concentrations of protein; from 6% aqueous silk fibroin solution a biofilm was prepared by using 1ml of the silk solution the amount of protein was 0.0297 g/ml, which it is 2.97 % w/v.                  .                                    Table 3.1: Silk fibroin biofilms samples.

| Samples | C7H10N2O2 Crosslinker volume | SF Volume & Concentration | Ultraviolet (UV) Wavelength |
| --- | --- | --- | --- |
| SS1 | 0µl | 2 ml Silk Fibroin Solution 3% | Short wave (254nm) |
| SS2 | 25µl |  |  |
| SS3 | 50µl |  |  |
| SS4 | 125µl |  |  |
| SS5 | 150µl |  |  |
| SL1 | 0 µl | 2 ml Silk Fibroin Solution 3% | Long wave (365nm) |
| SL2 | 25µl |  |  |
| SL3 | 50µl |  |  |
| SL4 | 125µl |  |  |
| SL5 | 150µl |  |  |

The prepared SF / N, N’ methylene diacrylamide biofilms are stable in toluene and acetone, and after treatment with methanol, their resistance to water treatment increases dramatically resulting in no obvious signs of dissolution observed after water treatment.

3.1 Swelling Test

The swelling test results for samples which were prepared in different reaction conditions with ABS or PBS solutions were discussed in this section.  The human physiological fluids pH range is change in between pH = 1 to 9, and human gastric fluid has approximately 1.2 pH value, gastrointestinal juice pH value is approximately 7.4, respectively. To estimate swelling behavior of biofilms in vitro conditions, SF/N, N’ methyelene diacrylamide biofilms were soaked in 40 ml of ABS and PBS solutions separately at 37oC and their behavior were evaluated. The swelling ratios of biofilms were different depending on the amount of crosslinker and wave length. In contrast, after a period of time samples were reached the equilibrium swelling ratio no matter which buffer solution was used. The swelling data were shown in the Tables 3.2, 3.5, 3.8, 3.11.

Figure 3.1: Swelling test for SF biofilms with ABS and PBS.

3.1.1 Swelling test for SF biofilms UV-Short wave with ABS

Table 3.2: Swelling test values of SF biofilms UV-Short wave with ABS (pH = 1.2)

| Time (Hours) | SS1 weight | SS2 weight | SS3 weight | SS4 weight | SS5 weight |
| --- | --- | --- | --- | --- | --- |
| 0 | 12.5 | 12.3 | 12.1 | 11.9 | 12.2 |
| 0.25 | 27.7 | 24.8 | 22.5 | 20.32 | 18.97 |
| 0. 5 | 28.3 | 25.7 | 23.98 | 21.11 | 20 |
| 0.75 | 33.2 | 27.73 | 24.32 | 22 | 20.89 |
| 1 | 36.1 | 29.99 | 25.61 | 23.41 | 21.34 |
| 1.5 | 38 | 33.76 | 27.41 | 24.98 | 22.10 |
| 2 | 40.12 | 35.21 | 28 | 26.12 | 22.99 |
| 24 | 41.8 | 36 | 29.53 | 27.63 | 23.5 |
| 48 | 42.2 | 37.2 | 31.43 | 28.79 | 24.38 |
| 96 | 43.9 | 39.11 | 32.1 | 29 | 26 |
| 120 | 44.2 | 40.31 | 32.4 | 29.3 | 26.43 |
| 144 | 44.8 | 40.85 | 32.6 | 29.7 | 26.79 |

Figure 3.2: Swelling test values for SF biofilms UV-Short wave with ABS.

The swelling test results showed that the samples without or with little amount of crosslinker swelled more than the samples with greater amount of crosslinker as shown in Table 3.2, Fig.3.2. As the amount of N, N’ methylene diacrylamide increases the crosslinking ratio also increases and the swelling ratio decreases. They are inversely proportional to each other.

Table 3.3: Swelling standard deviation for SF biofilms UV-Short wave with ABS.

| Samples | Total Numbers | Mean | Standard deviation | Variance(Standard deviation) | Population Standard deviation | Variance(Population Standard deviation) |
| --- | --- | --- | --- | --- | --- | --- |
| SS1 | 12 | 36.06833 | 9.47901 | 89.85167 | 9.07546 | 82.36403 |
| SS2 | 12 | 31.91333 | 8.29115 | 68.74321 | 7.93817 | 63.01461 |
| SS3 | 12 | 26.83167 | 5.83001 | 33.98898 | 5.58181 | 31.15656 |
| SS4 | 12 | 24.52167 | 5.19215 | 26.95843 | 4.97111 | 24.7119 |
| SS5 | 12 | 22.1325 | 4.02437 | 16.19558 | 3.85304 | 14.84595 |

Figure 3.3: Normal distribution for SF Biofilms UV-Short wave with ABS.

Standard deviation used to show how much variation or dispersion exists from the average (mean), or expected value. A low standard deviation indicates that the data points tend to be very close to the mean and high standard deviation indicates that the data points are spread out over a large range of values and the standard deviation calculated by equations number 4, 5, 6. According to the results of the standard deviation of silk fibroin biofilms UV-Short wave with ABS swelling as showed in Table 3.3 and Figure 3.3, the sample SS5 has the lowest standard deviation value and mean. SS5 was prepared with 150 µl of C7H10N2O2 cross linker. The sample SS1 which was prepared by without crosslinker has the highest standard deviation value and mean.

(4)

PSD =                                                                                  (5)

Variance = SD2                                                                                                                                                     (6)

Where:

SD = Standard Deviation

PSD= Population Standard Deviation

∑ = sum of

X= Individual score

M= Mean of the scores

N = Sample size (Number of scores)

The statistical results indicated that the stability of biofilms improved as the crosslinker amount increases during the synthesis. More crosslinked biofilms are more stable and swell less ABS. However, they reached at the equilibrium swelling ratio approximately at the same value.

Table 3.4: Swelling ratios for SF biofilms UV-Short wave with ABS.

| Time(Hours) | SS1 weight | SS2 weight | SS3 weight | SS4 weight | SS5 weight |
| --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.25 | 121.6 | 101.62 | 85.95 | 70.75 | 55.49 |
| 0. 5 | 126.4 | 108.94 | 89.18 | 77.39 | 63.93 |
| 0.75 | 165.6 | 125.44 | 100.99 | 84.87 | 71.22 |
| 1 | 188.8 | 143.82 | 111.65 | 96.72 | 74.91 |
| 1.5 | 204 | 174.47 | 126.52 | 109.91 | 81.14 |
| 2 | 220.96 | 186.26 | 131.40 | 119.49 | 88.44 |
| 24 | 234.4 | 192.68 | 144.04 | 132.18 | 92.62 |
| 48 | 237.6 | 202.43 | 159.75 | 141.93 | 99.83 |
| 96 | 251.2 | 217.96 | 165.28 | 143.69 | 113.11 |
| 120 | 253.6 | 227.72 | 167.76 | 146.21 | 116.63 |
| 144 | 258.4 | 232.11 | 169.42 | 149.57 | 119.59 |

Figure 3.4: Swelling ratios of SF biofilms UV-Short wave with ABS.

The swelling ratios were determined by using equation (1) and shown on Table 3.4 and Fig 3.4. For the acid buffer solution (pH = 1.2) sample which was pure silk fibroin biofilm increase in terms of swelling until it reached to its equilibrium swelling ratio value. However, it had the highest swelling ratio compared to the low crosslinked silk fibroin biofilm with the highly crosslinked silk fibroin biofilms. These indicate that as the crosslinker content increases in the biofilm the equilibrium swelling ratio decreases.

3.1.2 Swelling Test for Biofilms UV-Long wave (365nm) with ABS

The same swelling test procedure was applied to the samples which were prepared by UV long wavelength (365 nm). The biofilms prepared at short wavelength had an effect on the swelling ratios which was inversely proportional to the crosslinker. By comparing with the biofilms prepared by long UV wavelengths, they had a slower swelling and their final swelling ratio surpasses all the other biofilms prepared at long wavelength. This was related with the crosslink ratio of the UV-photo polymerization reaction.  As the crosslink ratio increases biofilms becomes messier and pore sizes were decreased. As the results were shown on Table 3.5 and Fig 5.3

Table 3.5: Swelling test values of SF biofilms UV-Long wave with ABS.

| Time(Hours) | SL1(w) | SL2(w) | SL3(w) | SL4(w) | SL5(w) |
| --- | --- | --- | --- | --- | --- |
| 0 | 14.3 | 14.6 | 13.8 | 14.1 | 13.9 |
| 0.25 | 32.11 | 27.7 | 24.2 | 22 | 19.4 |
| 0. 5 | 33.4 | 29.2 | 25.1 | 22.9 | 20.7 |
| 0.75 | 34.3 | 30.8 | 25.9 | 23.6 | 22.6 |
| 1 | 35.9 | 32 | 26.4 | 24.9 | 23.4 |
| 1.5 | 37.3 | 33.9 | 27.1 | 25.1 | 24 |
| 2 | 39.1 | 34.7 | 29.5 | 26.9 | 25.3 |
| 24 | 40.8 | 35.2 | 30.4 | 27.5 | 26 |
| 48 | 45.9 | 39.7 | 31.9 | 28.3 | 26.9 |
| 96 | 46.3 | 41.6 | 33.3 | 29.9 | 27.5 |
| 120 | 46.6 | 42 | 33.9 | 30.7 | 28 |
| 144 | 46.9 | 42.4 | 34.2 | 31 | 28.5 |

Figure 3.5: Swelling values of SF biofilms UV-Long wave with ABS.

Table 3.6: Swelling standard deviation for SF biofilms UV-Long wave with ABS.

| Samples | Total Numbers | Mean | Standard deviation | Variance(Standard deviation) | Population Standard deviation | Variance(Population Standard deviation) |
| --- | --- | --- | --- | --- | --- | --- |
| SL1 | 12 | 37.7425 | 9.18921 | 84.44149 | 8.79799 | 77.4047 |
| SL2 | 12 | 33.65 | 7.85441 | 61.69182 | 7.52003 | 56.55083 |
| SL3 | 12 | 27.9583 | 5.7078 | 32.57902 | 5.46481 | 29.8641 |
| SL4 | 12 | 25.575 | 4.70476 | 22.13477 | 4.50447 | 20.29021 |
| SL5 | 12 | 23.85 | 4.25024 | 18.06455 | 4.0693 | 16.55917 |

Figure 3.6: Normal distribution Biofilms UV-Long waves with ABS.

Table 3.7: Swelling test ratios of the SF biofilms UV-Long with ABS.

| Time(Hours) | SL1(w) | SL2(w) | SL3(w) | SL4(w) | SL5(w) |
| --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.25 | 124.54 | 89.72 | 75.36 | 56.02 | 39.56 |
| 0. 5 | 133.56 | 100 | 81.88 | 62.41 | 48.92 |
| 0.75 | 139.86 | 110.95 | 87.68 | 67.37 | 62.58 |
| 1 | 151.04 | 119.17 | 91.30 | 76.59 | 68.34 |
| 1.5 | 160.83 | 132.19 | 96.37 | 78.01 | 72.66 |
| 2 | 173.42 | 137.67 | 113.76 | 90.78 | 82.01 |
| 24 | 185.31 | 141.09 | 120.28 | 95.03 | 87.05 |
| 48 | 220.97 | 171.91 | 131.15 | 100.70 | 93.52 |
| 96 | 223.77 | 184.93 | 141.30 | 112.05 | 97.84 |
| 120 | 225.87 | 187.67 | 145.65 | 117.77 | 101.43 |
| 144 | 227.97 | 190.41 | 147.82 | 119.85 | 105.03 |

Figure 3.7: Swelling test ratios of SF biofilms UV-Long wave with ABS.

The swelling ratios were determined by equation (1) in chapter 2. As shown on Table 3.7 and Fig 3.7. For the acid buffer solution (pH = 1.2) samples prepared under long UV wave length, the pure SF biofilm increase in terms of swelling until it reached to its final swelling ratio value. It had the highest swelling ratio compared to the low crosslinked SF biofilm and the highly crosslinked SF biofilms. These indicate that as the crosslinker content increases in the biofilm the equilibrium swelling ratio decreases.

3.1.3 Swelling Test for Biofilms UV-Short wave 254nm With PBS

In this section, the swelling test applied to SF biofilms at phosphate buffer solution with pH = 7.404,  which were prepared by UV-short wavelength and different amount of crosslinkers (C7H10N2O2) as shown on Table 3.8 and Figure 3.8

Figure 3.8: Swelling test for SF biofilms UV-short wave.

Table 3.8 Swelling values of SF biofilms UV-Short wave with PBS.

| Time(hours) | SS1(w) | SS2(w) | SS3(w) | SS4(w) | SS5(w) |
| --- | --- | --- | --- | --- | --- |
| 0 | 12.2 | 12.3 | 11.8 | 12.4 | 12 |
| 0.25 | 46.2 | 45.7 | 36.3 | 27.1 | 25.1 |
| 0. 5 | 49.4 | 46.9 | 37.8 | 30.5 | 28.1 |
| 0.75 | 53.3 | 49.2 | 41.9 | 34.1 | 30.9 |
| 1 | 57.1 | 52.1 | 45.3 | 36.6 | 33.1 |
| 1.5 | 59.3 | 54.2 | 48.4 | 38.9 | 35.3 |
| 2 | 61.6 | 57.2 | 52.2 | 43.3 | 38.1 |
| 2.5 | 62.1 | 59.5 | 54.2 | 46.7 | 41.3 |
| 3.5 | 62.6 | 60.1 | 56.5 | 47.1 | 43.8 |
| 24 | 65.2 | 61.2 | 57.6 | 47.5 | 45.5 |
| 48 | 65.5 | 63.3 | 58.5 | 49.5 | 46.9 |
| 96 | 65.9 | 63.8 | 58.9 | 50 | 47.4 |

Figure 3.9: Swelling test values of SF biofilms UV-Short wave with PBS.

Same swelling test procedure was applied to the samples which were prepared by UV - Short wavelength (254 nm) and the results were shown on Table 3.8 and Figure 3.9. The biofilms prepared at short wavelength, the swelling ratios value was inversely proportional to the amount of crosslinker. By comparing with the biofilms prepared by long UV wavelengths they had a slower swelling ratio and their final swelling ratios surpass all the other biofilms prepared at long wavelength. This was related with the crosslink ratio of the UV-photopolymerization reaction. As the crosslink ratio increases biofilms becomes messier and pore sizes were decreased.

Table 3.9: Standard deviation for SF biofilms UV-Short wave with PBS.

| Samples | Total Numbers | Mean | Standard deviation | Variance(Standard deviation) | Population Standard deviation | Variance(Population Standard deviation) |
| --- | --- | --- | --- | --- | --- | --- |
| SS1 | 12 | 55.03333 | 14.92785 | 222.84061 | 14.29233 | 204.27056 |
| SS2 | 12 | 52.125 | 13.99598 | 195.8875 | 13.40013 | 179.56354 |
| SS3 | 12 | 46.61667 | 13.56002 | 183.87424 | 12.98273 | 168.55139 |
| SS4 | 12 | 38.75833 | 11.40235 | 130.01356 | 10.91692 | 119.1791 |
| SS5 | 12 | 35.625 | 10.54343 | 111.16386 | 10.09456 | 101.90021 |

Figure 3.10: Normal distribution Biofilms UV-Short waves with PBS.

From table 3.9 and Fig. 3.10 showed the effect of crosslinker on the standard deviation and mean is inversely proportional with crosslinker amounts. The standard deviation value of the sample which prepared without crosslinker is 14.29, while, the standard deviation value of the sample which prepared with the highest crosslinker value 10.09.

Table 3.10: Swelling ratios of the SF biofilms UV-Short wave with PBS.

| Time(hours) | SS1(w) | SS2(w) | SS3(w) | SS4(w) | SS5(w) |
| --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.25 | 278.68 | 271.54 | 207.62 | 118.54 | 109.16 |
| 0. 5 | 304.91 | 281.30 | 220.33 | 145.53 | 134.16 |
| 0.75 | 336.88 | 300 | 255.08 | 175.37 | 157.5 |
| 1 | 368.03 | 323.57 | 283.89 | 195.16 | 175.83 |
| 1.5 | 386.06 | 340.65 | 310.16 | 213.70 | 194.16 |
| 2 | 404.91 | 365.04 | 342.37 | 249.19 | 217.5 |
| 2.5 | 409.01 | 383.73 | 359.32 | 276.61 | 244.16 |
| 3.5 | 413.11 | 388.61 | 378.81 | 279.83 | 265.14 |
| 24 | 434.42 | 397.56 | 388.13 | 283.06 | 279.16 |
| 48 | 436.88 | 414.32 | 395.76 | 299.19 | 290.83 |
| 96 | 440 | 418.93 | 399.15 | 303.22 | 295.65 |

Figure 3.11: Swelling ratios of SF biofilms UV-Short wave with PBS.

This test also demonstrate the effect of crosslinker on the swelling process as well as comparing the difference between the samples which prepared in different conditions. The results which showed in Table 3.10 and Figure 3.11 indicated that the samples prepared under UV- Short wave generally swelled more than the samples which were prepared under UV- Long wave.

3.1.4 Swelling Test for Biofilms UV-Long wave Length 365nm with PBS

Table 3.11: Swelling test values of SF biofilms UV-Long wave with PBS.

| Time(Hours) | SL1 | SL2 | SL3 | SL4 | SL5 |
| --- | --- | --- | --- | --- | --- |
| 0 | 14.1 | 14.5 | 13.9 | 14 | 14.2 |
| 0.25 | 48.8 | 46.4 | 37.5 | 31.8 | 30 |
| 0. 5 | 49.5 | 47.6 | 39 | 33.1 | 32.7 |
| 0.75 | 53.1 | 48.9 | 40.1 | 34 | 33.3 |
| 1 | 54.9 | 51.1 | 42.8 | 35.3 | 34.2 |
| 1.5 | 56.6 | 53.9 | 45.1 | 36.8 | 35.2 |
| 2 | 58.4 | 54.7 | 46.8 | 37.3 | 35.9 |
| 2.5 | 61.1 | 56 | 47.3 | 38 | 36.6 |
| 3.5 | 62.8 | 57.2 | 48.1 | 38.7 | 37.4 |
| 24 | 64 | 59.1 | 49.2 | 39.4 | 37.9 |
| 48 | 65.1 | 60.3 | 49.9 | 40.1 | 38.4 |
| 96 | 65.7 | 60.9 | 50.3 | 40.6 | 39 |

Figure 3.12: Swelling test for SF biofilms UV-Long wave with PBS.

Table 3.12: Swelling standard deviation for SF biofilms UV-Long wave with PBS.

| Samples | Total Numbers | Mean | Standard deviation | Variance(Standard deviation) | Population Standard deviation | Variance(Population Standard deviation) |
| --- | --- | --- | --- | --- | --- | --- |
| SL1 | 12 | 54.50833 | 13.98665 | 195.62629 | 13.39119 | 179.3241 |
| SL2 | 12 | 50.88333 | 12.44945 | 154.98879 | 11.91944 | 142.07306 |
| SL3 | 12 | 42.5 | 10.00545 | 100.10909 | 9.57949 | 91.76667 |
| SL4 | 12 | 34.925 | 7.15937 | 51.25659 | 6.85458 | 46.98521 |
| SL5 | 12 | 33.73333 | 6.6902 | 44.75879 | 6.40538 | 41.02889 |

Figure 3.13: Normal distribution for Biofilms UV-Long waves with PBS.

According to the results of the standard deviation of silk fibroin biofilms, UV-Short wave with PBS swelling as showed in Table 3.12 and Fig 3.13, the sample SS5 has the lowest standard deviation value and mean. SS5 was prepared with 150 µl of C7H10N2O2 crosslinker. The sample SS1which was prepared without crosslinker has the highest standard deviation value and mean.

Table 3.13: Swelling ratios of the SF biofilms UV-Long wave with PBS.

| Time(hours) | SL1 | SL2 | SL3 | SL4 | SL5 |
| --- | --- | --- | --- | --- | --- |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.25 | 246.09 | 220 | 169.78 | 127.14 | 111.26 |
| 0. 5 | 251.06 | 228.27 | 180.57 | 136.42 | 130.28 |
| 0.75 | 276.59 | 237.24 | 188.48 | 142.85 | 134.50 |
| 1 | 289.36 | 252.14 | 207.91 | 152.14 | 140.84 |
| 1.5 | 301.41 | 271.72 | 224.46 | 162.85 | 147.88 |
| 2 | 314.18 | 277.24 | 236.69 | 166.42 | 152.81 |
| 2.5 | 333.33 | 286.20 | 240.28 | 171.32 | 157.74 |
| 3.5 | 345.39 | 294.48 | 246.04 | 176.42 | 163.38 |
| 24 | 353.90 | 307.58 | 253.95 | 181.73 | 166.90 |
| 48 | 361.70 | 315.86 | 258.99 | 186.25 | 170.42 |
| 96 | 365.95 | 320 | 261.87 | 190 | 174.64 |

Figure 3.14: Swelling test ratios of SF biofilms UV-Long wave with PBS.

According to the results that showed in Table 3.13 and Fig 3.14 the effect of crosslinker was very clear. As the crosslinker amount increased the swelling ratio of the silk fibroin biofilm decreased.

As a result, swelling process showed high pH sensitivity. The SF / N, N’ methylene diacrylamide biofilms may be useful as covering membranes in implantation process or carriers in drug delivery system. The crosslinked silk fibroin biofilms were insoluble in water and acid.

3.2 Biodegradation test

The silk fibroin biofilms biodegradation test was done by using protease enzyme weight per volume ratio 0.3 g/ml. The biofilms were tested within the enzyme solution at 37oC as showed in Figure 3.15.

Figure 3.15: Biodegradation test for SF biofilms with protease enzyme.

3.2.1 Biodegradation test for biofilms UV-Short wave length with protease enzyme

Table 3.14: Biodegradation test for SF biofilms UV-Short wave with protease enzyme.

| Time(Hours) | SS1(w) | SS2(w) | SS3(w) | SS4(w) | SS5(w) |
| --- | --- | --- | --- | --- | --- |
| 0 | 60.12 | 60.43 | 59.97 | 59.69 | 60 |
| 0.25 | 55.23 | 56.74 | 57.61 | 58.98 | 59.54 |
| 0.5 | 52.64 | 54.59 | 55.99 | 57.84 | 58.89 |
| 0.75 | 49.69 | 52.71 | 54.79 | 56.81 | 57.84 |
| 1 | 47.19 | 50.21 | 52.91 | 55.5 | 56.10 |
| 1.5 | 44.11 | 48.32 | 51 | 54.93 | 55.76 |
| 2 | 38.65 | 43.95 | 48.42 | 52.32 | 53.00 |
| 2.3 | 34.23 | 38.12 | 45.39 | 48.15 | 50.90 |
| 3 | 31.38 | 36.69 | 43.00 | 46.12 | 48.01 |
| 5 | 22.13 | 29.31 | 38.64 | 40.93 | 42.99 |
| 20 | 16.98 | 21.10 | 29.99 | 35.19 | 38.12 |
| 21 | 5.19 | 9.18 | 17.16 | 25.09 | 28.37 |
| 23 | 0 | 0 | 9.23 | 17.91 | 20.14 |
| 26 | 0 | 0 | 0 | 9.36 | 15.77 |
| 30 | 0 | 0 | 0 | 0 | 6.01 |
| 48 | 0 | 0 | 0 | 0 | 0 |

Figure 3.16: Biodegradation test for silk fibroin biofilms UV-Short wave length.

The biodegradation test results for biofilms prepared by UV-Short wave length were shown on Table 3.14 and Figure 3.16. The results indicated that, as the crosslinker amount increased in the preparation of biofilms the biodegradation rate was decreased. The samples which prepared by  lowest amount of crosslinker (SS1, SS2, SS3) completely biodegraded within 26 hours, while the samples that were prepared with highest amount of crosslinker (SS4, SS5) did not biodegraded in 24 hours. All samples were completely biodegraded within 48 hours.

Table 3.15: Biodegradation Standard deviation for SF biofilms UV-Short wave.

| Samples | Total Numbers | Mean | Standard deviation | Variance(Standard deviation) | Population Standard deviation | Variance(Population Standard deviation) |
| --- | --- | --- | --- | --- | --- | --- |
| SS1 | 16 | 28.59625 | 22.28408 | 496.58041 | 21.57647 | 465.54414 |
| SS2 | 16 | 31.33438 | 22.94262 | 526.36359 | 22.21409 | 493.46586 |
| SS3 | 16 | 35.25625 | 22.49505 | 506.02742 | 21.78074 | 474.40071 |
| SS4 | 16 | 38.67625 | 21.46725 | 460.84281 | 20.78558 | 432.04014 |
| SS5 | 16 | 40.715 | 20.31888 | 412.85676 | 19.67367 | 387.05321 |

Figure 3.17: Biodegradation test standard deviation for SF biofilms UV-Short wave.

Table 3.16: Biodegradation test ratios for SF biofilms UV-Short wave.

| Time | SS1 | SS2 | SS3 | SS4 | SS5 |
| --- | --- | --- | --- | --- | --- |
| 0 | 100 | 100 | 100 | 100 | 100 |
| 0.25 | 91.86 | 93.89 | 96.06 | 98.81 | 99.23 |
| 0.5 | 87.55 | 90.33 | 93.36 | 96.81 | 98.15 |
| 0.75 | 82.65 | 87.22 | 91.36 | 95.17 | 96.47 |
| 1 | 78.49 | 83.08 | 88.22 | 93.06 | 93.52 |
| 1.5 | 73.36 | 79.96 | 85.04 | 92.02 | 92.93 |
| 2 | 64.28 | 72.72 | 80.74 | 87.65 | 88.33 |
| 2.3 | 56.93 | 63.08 | 75.68 | 80.66 | 84.83 |
| 3 | 52.19 | 60.71 | 71.70 | 77.26 | 80.01 |
| 5 | 36.80 | 48.50 | 64.42 | 86.57 | 71.65 |
| 20 | 28.24 | 34.91 | 50.00 | 58.95 | 63.53 |
| 21 | 8.63 | 15.19 | 28.61 | 42.03 | 47.28 |
| 23 | 0 | 0 | 15.39 | 30.00 | 33.56 |
| 26 | 0 | 0 | 0 | 15.68 | 26.28 |
| 30 | 0 | 0 | 0 | 0 | 10.01 |
| 48 | 0 | 0 | 0 | 0 | 0 |

Figure 3.18: Biodegradation test ratios for SF biofilms UV-Short wave.

The degradation test results for biofilms prepared by UV-Short wave length were shown on Table 3.16 and figure 3.18. The results indicated that, as the crosslinker amount increased in the preparation of biofilms the biodegradation rate was decreased.

3.2.2 Biodegradation test for biofilms UV-Long wave with protease enzyme

Table 3.17: Biodegradation test values for SF biofilms UV-Long wave.

| Time (Hours) | SL1 | SL2 | SL3 | SL4 | SL5 |
| --- | --- | --- | --- | --- | --- |
| 0 | 61.5 | 61.9 | 61.7 | 61.6 | 61 |
| 0.25 | 55.6 | 56.1 | 58.2 | 58.4 | 59.1 |
| 0.5 | 50.92 | 53.23 | 55.9 | 56.8 | 57.9 |
| 0.75 | 43.41 | 45.84 | 48.11 | 51.45 | 53.64 |
| 1 | 36 | 39.12 | 42.9 | 47.31 | 50.12 |
| 1.5 | 29.59 | 35.87 | 37.00 | 43.85 | 48.59 |
| 2 | 25.89 | 30.10 | 31.85 | 38.43 | 45.00 |
| 2.5 | 16.36 | 22.44 | 25.05 | 30.35 | 38.69 |
| 4 | 9.32 | 11.01 | 14.33 | 21.00 | 30.98 |
| 24 | 00.00 | 00 | 0 | 10.4 | 18.90 |
| 27 | 0 | 0 | 0 | 0 | 10.18 |
| 48 | 0 | 0 | 0 | 0 | 0 |

Figure 3.19: Biodegradation test values for SF biofilms UV-Long wave length.

The biodegradation test results for biofilms prepared by UV-Long wave length were shown on Table 3.17 and Figure 3.19. The results indicated that, as the crosslinker amount increased in the preparation of biofilms the biodegradation rate was decreased. The samples which prepared by  lowest amount of crosslinker (SL1, SL2, SL3) completely biodegraded within 24 hours, while the samples that were prepared with highest amount of crosslinker (SL4, S5) did not biodegraded in 24 hours. All samples were completely biodegraded within 48 hours.

Table 3.18: Biodegradation Standard deviation for SF biofilms UV-Long wave length.

| Samples | Total Numbers | Mean | Standard deviation | Variance(Standard deviation) | Population Standard deviation | Variance(Population Standard deviation) |
| --- | --- | --- | --- | --- | --- | --- |
| SL1 | 12 | 27.3825 | 22.46136 | 504.51282 | 21.50512 | 462.47009 |
| SL2 | 12 | 29.63417 | 22.80982 | 520.28795 | 21.83874 | 476.93062 |
| SL3 | 12 | 31.25333 | 23.29445 | 542.63144 | 22.30274 | 497.41216 |
| SL4 | 12 | 34.96583 | 22.39187 | 501.39586 | 21.43858 | 459.61287 |
| SL5 | 12 | 39.52667 | 20.26019 | 410.47546 | 19.39766 | 376.26917 |

Figure 3.20: Biodegradation Standard deviations for SF biofilms UV-Long wave.

Table 3.19: Biodegradation test ratios for SF biofilms UV-Long wave.

| Time | SL1 | SL2 | SL3 | SL4 | SL5 |
| --- | --- | --- | --- | --- | --- |
| 0 | 100 | 100 | 100 | 100 | 100 |
| 0.25 | 90.43 | 90.09 | 94.32 | 94.80 | 96.88 |
| 0.5 | 82.79 | 85.99 | 90.59 | 92.20 | 94.93 |
| 0.75 | 70.58 | 74.05 | 77.97 | 83.52 | 87.93 |
| 1 | 58.53 | 63.19 | 69.52 | 76.80 | 82.16 |
| 1.5 | 48.11 | 57.94 | 59.98 | 71.18 | 79.65 |
| 2 | 42.09 | 48.62 | 51.62 | 62.38 | 73.77 |
| 2.5 | 26.60 | 36.25 | 40.59 | 49.26 | 63.42 |
| 4 | 15.15 | 17.78 | 23.22 | 34.09 | 50.78 |
| 24 | 0 | 0 | 0 | 16.88 | 30.98 |
| 27 | 0 | 0 | 0 | 0 | 16.55 |
| 48 | 0 | 0 | 0 | 0 | 0 |

Figure 3.21: Biodegradation test ratios for SF biofilms UV-Long wave length.

The biodegradation ratio values were determined by using equation (2) in section 2. The results were shown in Table 3.19 and Figure 3.21 indicated that after half an hour from the initial time, the biodegradation rate was increased for all samples without considering the crosslinker effect. After 24 hours, SL1(without crosslinker), SL2 and SL3 which have small amount of  crosslinker were biodegraded completely while SL5 which had highest amount of crosslinker still keep about 30.98% from its own weight as shown in Table 3.19. In 48 hours, SL4 was also biodegraded, while SL5 still keep about 16.55% from its own weight. After 55 hours from the beginning the SL5 was also biodegraded completely. These results indicated that, the biodegradation rate can be easily controlled by the amount of crosslinker added to the reaction mixture. As the amount of crosslinker increases, it enhanced the formation of crosslinking sites and also β-sheet formation triggered. Structural control of the silk protein was also gained through physical crosslinks (β-sheets), resulting in roboust and stable thin material coating (Jiang et al, 2007).

3.3Scanning electron microscope (SEM) analyses

Figure 3.22: SEM analyses for SF biofilms without crosslinker.

Figure 3.23: SEM analyses for SF biofilms with 25µl crosslinker.

Figure 3.24 SEM analyses for SF biofilms with 50µl of crosslinker.

Figure 3.25: SEM analyses for SF biofilms with 125µl of crosslinker.

Figure 3.26: SEM analyses for SF biofilms with 150µl of crosslinker.

The SEM analyses showed that, the morphology of the silk fibroin biofilms have been changed as the amount of crosslinker (C7H10N2O2) varied within the preparation ratio. Different morphologies of the biofilms are attributed to the different modes of crosslinking, and β-sheet formation. The highly crosslinked regions are separated from each other by well-defined thick fibroin network due to the highest amount of crosslinker during the preparation. Fig. 3.26 with 150 µl of crosslinker content showing SEM images of the thick fibroin biofilm formed at 254 nm wave length.

The SEM micrographs for silk fibroin biofilms also showed the crosslinker effects on the surface smoothness. The SEM micrographs for silk fibroin biofilms which prepared under UV –Short wave 254nm and UV-Long wave 365 nm indicate that the silk fibroin biofilms useful in cell culturing due to the porous structure and enable to cells proliferation and growth on the biofilm.

3.4 X-Ray Diffraction (XRD) Analyses

Table 3.20: X-Ray diffraction analyses of silk fibroin and silk fibroin biofilms prepared by UV-Short wave at 254nm.

| samples | Strongest peak no. | 2 theta (deg) | d(A) | I/II | FWHM (deg) | Intensity (counts) | Integrated Int.(counts) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SFX(silk fibroin biofilms) | 16 | 20.4200 | 4.345 | 100 | 0 | 111 | 0 |
|  | 15 | 19.4800 | 4.553 | 86 | 0 | 95 | 0 |
|  | 14 | 21.1800 | 4.191 | 86 | 0 | 95 | 0 |
| Raw silk fibroin | 6 | 11.620 | 7.609 | 100 | 2.240 | 37 | 3290 |
|  | 11 | 20.560 | 4.316 | 76 | 2.100 | 28 | 2493 |
|  | 5 | 10.46 | 8.4505 | 68 | 1.200 | 25 | 1099 |
| SFS(silk fibroin scaffolds) | 7 | 12.580 | 7.030 | 100 | 1.1600 | 17 | 1577 |
|  | 15 | 20.500 | 4.328 | 100 | 1.400 | 17 | 1133 |
|  | 4 | 4.120 | 9.688 | 94 | 1.040 | 16 | 1003 |

The X-Ray diffraction test results were summarized in Table 3.20. In the crosslinked samples weaker crystalline appeared at 12.58, 20.50, and 9.120. The raw silk fibroin samples gives three characteristic crystallinity peaks at 2 theta = 20.42, 19.48 and 21.180. The crystalline structure was affected as the amount of crosslinker increased in silk fibroin/ crosslinker ratio.

Figure 3.27: Comparison of (Data: S1) raw SF XDR pattern. (Data: S2) XDR pattern of SF scaffold prepared by freeze drying technique at 80C. (Data: S3) SF biofilms which prepared by UV induced photo polymerization technique under homogeneous conditions.

The XDR analysis for silk fibroin biofilms showed that the degree of crystallinity and the crystalline structure were affected by structural formation processes such as cross linker, the crosslinker help to formation ordered structure of silk fibroin biofilms.

3.5 In-vitro Coagulation Time Test Analyses

In this study, for the first time to our knowledge we analyzed the effect of crosslinker C7H10N2O2 on SF biofilms prepared by UV-irradiation under homogenous condition for determining plasma coagulation. Data were detected by measuring the activated partial thromboplastin time (APTT), prothrombin time (PTT), and INR by STA Compact Hemostasis System equipment, Stago, US. The results of in-vitro coagulation time tests were shown on the Table 3.21.

Table 3.21: The results of in-vitro coagulation time tests.

| Sample | ActPT% | PTT | INR | APTT |
| --- | --- | --- | --- | --- |
| Healthy Blood | 114 | 0.93 | 12.7 | 25.9 |
| SF Biofilm | 113 | 0.93 | 12.9 | 26.1 |
| Crosslinked SF Biofilm | 110 | 1.01 | 13.4 | 26.3 |

The in-vitro coagulation time tests have been applied and results showed that the Prothrombin Time (PTT), APPT of the crosslinked SF biofilms prepared by casting method were higher than SF biofilms. This indicated that crosslinking ratio had an effect on the blood clotting period of time. As the β-sheet formation enhanced by adding crosslinker in the reaction mixture, the PTT and APPT were increased and improve the blood compatibility property of the biofilm. The biofilm exhibit high blood compatibility property making them good candidates as biomedical material for blood contacting devices.

3.6 In-vitro Platelet Adhesion Analyses with Peripheric Seaming Method

Figure 3.30: The electron microscope micrograph of SF crosslinked biofilm.

The in vitro peripheric seaming method was applied to analyzed platelet adhesion property of the prepared biofilms. The electron microscope micrograph of SF/ N, N’ methylene diacrylamide biofilms demonstrated that no platelet adhere on the surface of the biomaterial, as shown on Figure 3.30. The results indicated that the crosslinked SF biofilms could be considered as ideal candidates for biomedical applications.

Different forms of silk fibroin biofilms were prepared by UV induced photopolymerization technique under homogeneous conditions at short wave length 254 nm and long wave length 365 nm. The effects of crosslinker concentration, pH, and UV wave length were indicated on the physiochemical properties of the silk fibroin biofilms. Methanol treatment fixed the silk fibroin biofilms secondary structure. Due to the silk fibroin biofilms properties such as biocompatibility, biodegradability, and swelling gives the preference for silk fibroin biofilms to use it in the biomedical applications.

CHAPTER 4 CONCLUSIONS

Different forms of silk fibroin biofilms were prepared by UV induced photo polymerization technique under homogeneous conditions at short wave length 254 nm and long wave length 365 nm. The effects of crosslinker concentration, UV-wave length and different pH values were examined and their effects on the physiochemical properties of the silk fibroin biofilms have been shown. These films were characterized by SEM and XRD analysis and because of the formation of microstructure with crystalline β-sheets they improve their resistivity towards biodegradation and swelling properties can be controllable by the amount of crosslinker added to the reaction mixture.   N, N’ methyelene diacrylamide triggers the conformational transition of fibroin from random coil to β-sheet structure and hence fibroin film formation. One of the unique features is the blood compatibility property that allows to resists blood clotting and platelet adhesion.

These regenerated SF / N, N’ methylene diacrylamide biofilms with their potential biocompatibility and physicochemical properties should provide value to a number of biomedical devices in the future.

References

Alessandrino, A., Marelli, B., Arosio, C., Fare, S., Tanzi, M. C., & Freddi, G. (2008). Electrospun silk fibroin mats for tissue engineering. Engineering in life sciences, 8(3), 219-225. http://onlinelibrary.wiley.com/doi/10.1002/elsc.200700067/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Altman, G. H., Diaz, F., Jakuba, C., Calabro, T., Horan, R. L., Chen, J., ...& Kaplan, D. L. (2003). Silk-based biomaterials. Biomaterials, 24(3), 401-416.

Altman, G. H., Horan, R. L., Lu, H. H., Moreau, J., Martin, I., Richmond, J. C., & Kaplan, D. L. (2002). Silk matrix for tissue engineered anterior cruciate ligaments. Biomaterials, 23(20), 4131-4141. http://www.sciencedirect.com/science/article/pii/S0142961202001564

Altman, G. H., Horan, R. L., Lu, H. H., Moreau, J., Martin, I., Richmond, J. C., & Kaplan, D. L. (2002). Silk matrix for tissue engineered anterior cruciate ligaments. Biomaterials, 23(20), 4131-4141. http://www.sciencedirect.com/science/article/pii/S0142961202001564

Baimark, Y., Srihanam, P., Srisuwan, Y., & Phinyocheep, P. (2010). Preparation of porous silk fibroin microparticles by a water‐in‐oil emulsification‐diffusion method. Journal of Applied Polymer Science, 118(2), 1127-1133. http://onlinelibrary.wiley.com/doi/10.1002/app.32506/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Benfenati, V., Pistone, A., Sagnella, A., Stahl, K., Camassa, L., Gomis-Perez, C., ... & Muccini, M. (2012). Silk fibroin films are a bio-active interface for neuroregenerative medicine. Journal of applied biomaterials & functional materials, 10(3), 315-323.

Bray, L. J., George, K. A., Ainscough, S. L., Hutmacher, D. W., Chirila, T. V., & Harkin, D. G. (2011). Human corneal epithelial equivalents constructed on< i> Bombyx mori</i> silk fibroin membranes. Biomaterials, 32(22), 5086-5091. http://www.sciencedirect.com/science/article/pii/S0142961211003668

Cao, Z., Chen, X., Yao, J., Huang, L., & Shao, Z. (2007). The preparation of regenerated silk fibroin microspheres. Soft Matter, 3(7), 910-915. http://pubs.rsc.org/en/content/articlelanding/2007/sm/b703139d#!divAbstract

Correia, C., Bhumiratana, S., Leping, Y., Oliveira, A. L., Gimble, J. M., Kaplan, D. L., ... & Reis, R. L. The Influence of Silk Fibroin 3D Scaffold Composition For In Vitro Bone Tissue Engineering. Bone, 70, 90.

Dobb, M. G., Fraser, R. D. B., & Macrae, T. P. (1967). The fine structure of silk fibroin. The Journal of cell biology, 32(2), 289-295. http://jcb.rupress.org/content/32/2/289.abstract

Enomoto, S., Sumi, M., Kajimoto, K., Nakazawa, Y., Takahashi, R., Takabayashi, C., ... & Sata, M. (2010). Long-term patency of small-diameter vascular graft made from fibroin, a silk-based biodegradable material. Journal of Vascular Surgery, 51(1), 155-164. http://dx.doi.org/10.1016/j.jvs.2009.09.005

Freddi, G., Anghileri, A., Sampaio, S., Buchert, J., Monti, P., & Taddei, P. (2006). Tyrosinase-catalyzed modification of  Bombyx mori silk fibroin: Grafting of chitosan under heterogeneous reaction conditions. Journal of biotechnology, 125(2), 281-294. http://www.sciencedirect.com/science/article/pii/S0168165606001970

Freddi, G., Romanò, M., Massafra, M. R., & Tsukada, M. (1995). Silk fibroin/cellulose blend films: Preparation, structure, and physical properties. Journal of applied polymer science, 56(12), 1537-1545. http://onlinelibrary.wiley.com/doi/10.1002/app.1995.070561203/abstract

Freddi, G., Tsukada, M., & Beretta, S. (1999). Structure and physical properties of silk fibroin/polyacrylamide blend films. Journal of applied polymer science, 71(10), 1563-1571.

Gil, E. S., & Hudson, S. M. (2007). Effect of silk fibroin interpenetrating networks on swelling/deswelling kinetics and rheological properties of poly (N-isopropylacrylamide) hydrogels. Biomacromolecules, 8(1), 258-264. http://pubs.acs.org/doi/abs/10.1021/bm060543m

Gil, E. S., Frankowski, D. J., Spontak, R. J., & Hudson, S. M. (2005). Swelling behavior and morphological evolution of mixed gelatin/silk fibroin hydrogels. Biomacromolecules, 6(6), 3079-3087.http://pubs.acs.org/doi/abs/10.1021/bm050396c

Gotoh, Y., Tsukada, M., Baba, T., & Minoura, N. (1997). Physical properties and structure of poly (ethylene glycol)-silk fibroin conjugate films. Polymer, 38(2), 487-490. http://www.sciencedirect.com/science/article/pii/S0032386196006659

Gupta, V., Aseh, A., Ríos, C. N., Aggarwal, B. B., & Mathur, A. B. (2009). Fabrication and characterization of silk fibroin-derived curcumin nanoparticles for cancer therapy. International journal of nanomedicine, 4, 115. http://www.ncbi.nlm.nih.gov/pmc/articles/PMC2720745/

Hines, D. J., & Kaplan, D. L. (2011). Mechanisms of controlled release from silk fibroin films. Biomacromolecules, 12(3), 804-812.http://pubs.acs.org/doi/abs/10.1021/bm101421r

Hofmann, S., Wong Po Foo, C. T., Rossetti, F., Textor, M., Vunjak-Novakovic, G., Kaplan, D. L., ... & Meinel, L. (2006). Silk fibroin as an organic polymer for controlled drug delivery. Journal of Controlled Release, 111(1), 219-227. http://www.sciencedirect.com/science/article/pii/S0168365905007327

Hu, K., Lv, Q., Cui, F. Z., Feng, Q. L., Kong, X. D., Wang, H. L., ... & Li, T. (2006). Biocompatible fibroin blended films with recombinant human-like collagen for hepatic tissue engineering. Journal of bioactive and compatible polymers, 21(1), 23-37. http://jbc.sagepub.com/content/21/1/23.short

Hu, Y., Zhang, Q., You, R., Wang, L., & Li, M. (2012). The relationship between secondary structure and biodegradation behavior of silk fibroin scaffolds. Advances in Materials Science and Engineering. http://www.hindawi.com/journals/amse/2012/185905/

Imsombut, T., Srisuwan, Y., Srihanam, P., & Baimark, Y. (2010). Genipin-cross-linked silk fibroin microspheres prepared by the simple water-in-oil emulsion solvent diffusion method. Powder Technology, 203(3), 603-608. http://www.sciencedirect.com/science/article/pii/S0032591010003359

Jiang, C., Wang, X., Gunawidjaja, R., Lin, Y. H., Gupta, M. K., Kaplan, D. L., ...& Tsukruk, V. V. (2007). Mechanical properties of robust ultrathin silk fibroin films. Advanced functional materials, 17(13), 2229-2237. http://onlinelibrary.wiley.com/doi/10.1002/adfm.200601136/abstract

Jin, H. J., Chen, J., Karageorgiou, V., Altman, G. H., & Kaplan, D. L. (2004). Human bone marrow stromal cell responses on electrospun silk fibroin mats. Biomaterials, 25(6), 1039-1047. http://www.sciencedirect.com/science/article/pii/S0142961203006094.

Jin, H. J., Fridrikh, S. V., Rutledge, G. C., & Kaplan, D. L. (2002). Electrospinning Bombyx mori silk with poly (ethylene oxide). Biomacromolecules, 3(6), 1233-1239.http://pubs.acs.org/doi/abs/10.1021/bm025581u

Jin, H. Y., Yin, H., An, Y., Liu, Y., Wang, D. P., Liu, J., & Liu, X. (2012). Study on Biocompatibility of  Post-Irradiated Silk Fibroin In Vitro. Advanced Materials Research, 535, 2357-2360. http://www.scientific.net/AMR.535-537.2357

Kasoju, N., & Bora, U. (2012). Silk Fibroin in Tissue Engineering. Advanced healthcare materials, 1(4), 393-412. http://onlinelibrary.wiley.com/doi/10.1002/adhm.201200097/full

Korte, W., Clarke, S., & Lefkowitz, J. B. (2000). Short activated partial thromboplastin times are related to increased thrombin generation and an increased risk for thromboembolism. American journal of clinical pathology, 113(1), 123-127. http://ajcp.ascpjournals.org/content/113/1/123.short

Kundu, J., Chung, Y. I., Kim, Y. H., Tae, G., & Kundu, S. C. (2010). Silk fibroin nanoparticles for cellular uptake and control release. International journal of pharmaceutics, 388(1), 242-250.

Kweon, H. Y., Woo, S. O., & Jo, Y. Y. (2010). Preparation and Characterization of Silk Fibroin Nanoparticles. International Journal of Industrial Entomology, 20(1), 25-28. http://www.papersearch.net/view/detail.asp?detail_key=0n601646

Kweon, H., Ha, H. C., Um, I. C., & Park, Y. H. (2001). Physical properties of silk fibroin/chitosan blend films. Journal of applied polymer science, 80(7), 928-934. http://onlinelibrary.wiley.com/doi/10.1002/app.1172/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Lawrence, B. D., Marchant, J. K., Pindrus, M. A., Omenetto, F. G., & Kaplan, D. L. (2009). Silk film biomaterials for cornea tissue engineering. Biomaterials, 30(7), 1299-1308. http://www.sciencedirect.com/science/article/pii/S0142961208009095

Lawrence, B. D., Pan, Z., Weber, M. D., Kaplan, D. L., & Rosenblatt, M. I. (2012). Silk film culture system for in vitro analysis and biomaterial design. Journal of visualized experiments: JoVE, (62). http://www.ncbi.nlm.nih.gov/pmc/articles/PMC3466641/

Liu, H., Ge, Z., Wang, Y., Toh, S. L., Sutthikhum, V., & Goh, J. C. (2007). Modification of sericin‐free silk fibers for ligament tissue engineering application. Journal of Biomedical Materials Research Part B: Applied Biomaterials, 82(1), 129-138. http://onlinelibrary.wiley.com/doi/10.1002/jbm.b.30714/full

Lu, Q., Wang, X., Hu, X., Cebe, P., Omenetto, F., & Kaplan, D. L. (2010). Stabilization and release of enzymes from silk films. Macromolecular bioscience, 10(4), 359-368. http://onlinelibrary.wiley.com/doi/10.1002/mabi.200900388/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Luangbudnark, W., Viyoch, J., Laupattarakasem, W., Surakunprapha, P., & Laupattarakasem, P. (2012). Properties and biocompatibility of chitosan and silk fibroin blend films for application in skin tissue engineering. The Scientific World Journal, 2012. http://www.hindawi.com/journals/tswj/2012/697201/abs/

Ma, X., Cao, C., & Zhu, H. (2006). The biocompatibility of silk fibroin films containing sulfonated silk fibroin. Journal of Biomedical Materials Research Part B: Applied Biomaterials, 78(1), 89-96. http://onlinelibrary.wiley.com/doi/10.1002/jbm.b.30466/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Mathur, A. B., & Gupta, V. (2010). Silk fibroin-derived nanoparticles for biomedical applications. Nanomedicine, 5(5), 807-820. http://www.futuremedicine.com/doi/abs/10.2217/nnm.10.51

Moraes, M. A. D., Nogueira, G. M., Weska, R. F., & Beppu, M. M. (2010). Preparation and characterization of insoluble silk fibroin/chitosan blend films. Polymers, 2(4), 719-727.http://www.mdpi.com/2073-4360/2/4/719

Motta, A., Maniglio, D., Migliaresi, C., Kim, H. J., Wan, X., Hu, X., & Kaplan, D. L. (2009). Silk fibroin processing and thrombogenic responses. Journal of Biomaterials Science, Polymer Edition, 20(13), 1875-1897.

Myung, S. J., Kim, H. S., Kim, Y., Chen, P., & Jin, H. J. (2008). Fluorescent silk fibroin nanoparticles prepared using a reverse microemulsion. Macromolecular Research, 16(7), 604-608. http://link.springer.com/article/10.1007/BF03218567#page-1

Nagarkar, S., Nicolai, T., Chassenieux, C., & Lele, A. (2010). Structure and gelation mechanism of silk hydrogels. Physical Chemistry Chemical Physics, 12(15), 3834-3844. http://pubs.rsc.org/en/content/articlelanding/2010/cp/b916319k#!divAbstract.

Oh, S. H., & Lee, J. H. (2013). Hydrophilization of synthetic biodegradable polymer scaffolds for improved cell/tissue compatibility. Biomedical Materials, 8(1), 014101. http://iopscience.iop.org/1748-605X/8/1/014101

Patel, A. A., Thakar, R. G., Chown, M., Ayala, P., Desai, T. A., & Kumar, S. (2010). Biophysical mechanisms of single-cell interactions with microtopographical cues. Biomedical microdevices, 12(2), 287-296. http://link.springer.com/article/10.1007/s10544-009-9384-7#page-1

Pérez‐Rigueiro, J., Elices, M., Llorca, J., & Viney, C. (2001). Tensile properties of silkworm silk obtained by forced silking. Journal of Applied Polymer Science, 82(8), 1928-1935. http://onlinelibrary.wiley.com/doi/10.1002/app.2038/full

Phillips, D. M., Drummy, L. F., Conrady, D. G., Fox, D. M., Naik, R. R., Stone, M. O., ...& Mantz, R. A. (2004). Dissolution and regeneration of Bombyx mori silk fibroin using ionic liquids. Journal of the American chemical society, 126(44), 14350-14351. http://pubs.acs.org/doi/abs/10.1021/ja046079f

Rajkhowa, R., Levin, B., Redmond, S. L., Li, L. H., Wang, L., Kanwar, J. R., ... & Wang, X. (2011). Structure and properties of biomedical films prepared from aqueous and acidic silk fibroin solutions. Journal of Biomedical Materials Research Part A, 97(1), 37-45. http://onlinelibrary.wiley.com/doi/10.1002/jbm.a.33021/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Reddy, N., Jiang, Q., & Yang, Y. (2012). Biocompatible Natural Silk Fibers from Argema mittrei. Journal of Biobased Materials and Bioenergy, 6(5), 558-563. http://www.ingentaconnect.com/content/asp/jbmb/2012/00000006/00000005/art00006

S. Prasong, S. Wilaiwan and K. Nualchai. (2001).Structure and Thermal Characteristics of Bombyx mori Silk Fibroin Films: Effect of Different Organic Solvents”, International Journal of Chemical Technology 2(1): 21-27, 2010 ISSN 1996-3416.

Sah, M. K., & Pramanik, K. (2010). Regenerated Silk Fibroin from B. mori Silk Cocoon for Tissue Engineering Applications. Int. J. Environ. Sci. Technol, 1, 404-408.

Sashina, E. S., Bochek, A. M., Novoselov, N. P., & Kirichenko, D. A. (2006). Structure and solubility of natural silk fibroin. Russian journal of applied chemistry, 79(6), 869-876. http://link.springer.com/article/10.1134/S1070427206060012#page-1

Sashina, E. S., Dubkova, O. I., Novoselov, N. P., Goralsky, J. J., Szynkowska, M. I., Lesniewska, E., ... & Strobin, G. (2009). Silver nanoparticles on fibers and films of Bombyx mori silk fibroin. Russian Journal of Applied Chemistry, 82(6), 974-980. http://link.springer.com/article/10.1134/S1070427209060081#page-1

Serban, M. A., Panilaitis, B., & Kaplan, D. L. (2011). Silk fibroin and polyethylene glycol‐based biocompatible tissue adhesives. Journal of Biomedical Materials Research Part A,98(4),567-575. http://onlinelibrary.wiley.com/doi/10.1002/jbm.a.33149/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Sukigara, S., Gandhi, M., Ayutsede, J., Micklus, M., & Ko, F. (2004). Regeneration of Bombyx mori silk by electrospinning. Part 2. Process optimization and empirical modeling using response surface methodology. Polymer, 45(11), 3701-3708. http://www.sciencedirect.com/science/article/pii/S0032386104003131

Sukigara, S., Gandhi, M., Ayutsede, J., Micklus, M., &Ko, F. (2003). Regeneration of Bombyx mori silk by electrospinning: Part 1: processing parameters and geometric properties. Polymer,44(19),5721-5727. http://www.sciencedirect.com/science/article/pii/S0032386103005329

Sun, M., Zhou, P., Pan, L. F., Liu, S., & Yang, H. X. (2009). Enhanced cell affinity of the silk fibroin-modified PHBHHx material. Journal of Materials Science: Materials in Medicine, 20(8), 1743-1751. http://link.springer.com/article/10.1007/s10856-009-3739-8#page-1

Teo, W. E., & Ramakrishna, S. (2006). A review on electrospinning design and nanofibre assemblies. Nanotechnology, 17(14), R89. http://iopscience.iop.org/0957-4484/17/14/R01

Thomson, R. C., Wake, M. C., Yaszemski, M. J., & Mikos, A. G. (1995). Biodegradable polymer scaffolds to regenerate organs. In Biopolymers Ii (pp. 245-274). Springer Berlin Heidelberg.

Uebersax, L., Mattotti, M., Papaloïzos, M., Merkle, H. P., Gander, B., & Meinel, L. (2007). Silk fibroin matrices for the controlled release of nerve growth factor (NGF). Biomaterials, 28(30), 4449-4460.

Valluzzi, R., Gido, S. P., Muller, W., & Kaplan, D. L. (1999). Orientation of silk III at the air-water interface. International journal of biological macromolecules, 24(2), 237-242. http://www.sciencedirect.com/science/article/pii/S0141813099000021

Vasconcelos, A., Gomes, A. C., & Cavaco-Paulo, A. (2012). Novel silk fibroin/elastin wound dressings. ActaBiomaterialia, 8(8), 3049-3060. http://www.sciencedirect.com/science/article/pii/S1742706112001821

Vepari, C., & Kaplan, D. L. (2007). Silk as a biomaterial. Progress in polymer science, 32(8), 991-1007.http://www.sciencedirect.com/science/article/pii/S0079670007000731

Wenk, E., Wandrey, A. J., Merkle, H. P., & Meinel, L. (2008). Silk fibroin spheres as a platform for controlled drug delivery. Journal of Controlled Release, 132(1), 26-34. http://www.sciencedirect.com/science/article/pii/S0168365908004628

Xu, Y., Wang, Y., Jiao, Y., Zhang, C., & Li, M. (2011). Enzymatic degradation properties of silk fibroin film. Journal of Fiber Bioengineering and Informatics, 4(1), 35-41.

Yamaura, K., Kuranuki, N., Suzuki, M., Tanigami, T., & Matsuzawa, S. (1990). Properties of mixtures of silk fibroin/syndiotactic‐rich poly (vinyl alcohol). Journal of applied polymer science,41(9‐10),2409-2425. http://onlinelibrary.wiley.com/doi/10.1002/app.1990.070410941/abstract

Yan, L. P., Oliveira, J. M., Oliveira, A. L., Caridade, S. G., Mano, J. F., & Reis, R. L. (2012). Macro/microporous silk fibroin scaffolds with potential for articular cartilage and meniscus tissue engineering applications. ActaBiomaterialia, 8(1), 289-301. http://www.sciencedirect.com/science/article/pii/S1742706111004302

Yang, Y., Ding, F., Wu, J., Hu, W., Liu, W., Liu, J., & Gu, X. (2007). Development and evaluation of silk fibroin-based nerve grafts used for peripheral nerve regeneration. Biomaterials, 28(36), 5526-5535. http://www.sciencedirect.com/science/article/pii/S0142961207007053

Yeo, J. H., Lee, K. G., Lee, Y. W., & Kim, S. Y. (2003). Simple preparation and characteristics of silk fibroin microsphere. European Polymer Journal, 39(6), 1195-1199. http://www.sciencedirect.com/science/article/pii/S0014305702003592

Zang, M., Zhang, Q., Davis, G., Huang, G., Jaffari, M., Ríos, C. N., ... & Mathur, A. B. (2011). Perichondrium directed cartilage formation in silk fibroin and chitosan blend scaffolds for tracheal transplantation. ActaBiomaterialia, 7(9), 3422-3431. http://www.sciencedirect.com/science/article/pii/S1742706111002054

Zarkoob, S. (1998). Structure and morphology of regenerated silk nano-fibers produced by electrospinning (Vol. 1, p. 77). http://adsabs.harvard.edu/abs/1998PhDT........77Z

Zarkoob, S., Reneker, D. H., Ertley, D., Eby, R. K., & Hudson, S. D. (2000). U.S. Patent No. 6,110,590. Washington, DC: U.S. Patent and Trademark Office. http://onlinelibrary.wiley.com/doi/10.1002/elsc.200700067/abstract?deniedAccessCustomisedMessage=&userIsAuthenticated=false

Zhang, Y. Q., Shen, W. D., Xiang, R. L., Zhuge, L. J., Gao, W. J., & Wang, W. B. (2007). Formation of silk fibroin nanoparticles in water-miscible organic solvent and their characterization. Journal of Nanoparticle Research, 9(5), 885-900. http://link.springer.com/article/10.1007/s11051-006-9162-x#page-1

Zhao, Z., Chen, A., Li, Y., Hu, J., Liu, X., Li, J., ...& Zheng, Z. (2012). Fabrication of silk fibroin nanoparticles for controlled drug delivery. Journal of Nanoparticle Research, 14(4), 1-10. http://link.springer.com/article/10.1007/s11051-012-0736-5#page-1

Zhou, P. (2011). Degradable PHBHHx Modified by the Silk Fibroin for the Applications of Cardiovascular Tissue Engineering. ISRN Materials Science, 2011. http://www.hindawi.com/isrn/materials.science/2011/389872/

# Text boxes

Observed strongest peaks. Highly crystaline structure.

Observed strongest peaks. Less crystalline structure observed.

No strong peak observed. Amorphous structure